## Slide 1
Dr. Ahmed SOLIMAN Ph.D., P.Eng. (ON).
Associate Professor, Building Civil and Environmental Engineering Department
March 31St, 2025
EXPANDING THE APPLICATION OF RECYCLED CONCRETE AGGREGATES FOR ROAD CONSTRUCTION

## Slide 2
Recycled Concrete Aggregate
Demolition of Concrete Structure
Returned Concrete

## Slide 3
Recycled Concrete Aggregate
Demolition of Concrete Structure
Returned Concrete

## Slide 4
Recycled Concrete Aggregate

## Slide 5
Recycled Concrete Aggregate

## Slide 6
Bibliometric analysis of RCA Research
Construction practices and resource management
Engineering applications and performance metrics
Material properties and characterization

## Slide 7
Sampling RCA
 | Size range | Source description | Status
RCA 1 | 0 – 20 | Demolition Concrete and Ready-Mix Returns | TREATED
RCA 2 | 0 – 50 |  | 
RCA 3 | 0 – 31.5 | Bridge, culvert, concrete structure | 
RCA 4 | 0 – 56 |  | 
RCA 5 | 0 – 31.5 | Sidewalk and sub-pavement slab | 
RCA 6 | 0 – 50 | Demolition Concrete and Ready-Mix Returns | Not TREATED
Untreated RCA
Treated RCA

## Slide 8
Research Work
Key Aspects
Knowledge and Awareness
Current Practices
Implementation Barriers
Environmental Impact
Analysis Focus
Acceptance level
Implementation Challenges
Industry Recommendation
Future Implementation Strategies
Survey
Physical Properties
Visual Inspection
Sieve Analysis
Specific Gravity
Water Absorption
Bulk Density
Durability Test
Micro Deval
Washing Cycles Analysis
Infiltration Rate
Technical Evaluation

## Slide 9
Research Work
Physical Properties
Visual Inspection
Sieve Analysis
Specific Gravity
Water Absorption
Bulk Density
Durability Test
Micro Deval
Washing Cycles Analysis
Infiltration Rate
Technical Evaluation
Los Angelos Abrasion Test
Infiltration Rate
Washing Cycles
Standard Proctor Test
Sieve Analysis

## Slide 10
N.A.≈ 2.75
The treated recycled concrete aggregate had an acceptable Specific Gravity
RCA: 2.4-2.5

## Slide 11
The treated recycled concrete aggregate showed a significantly lower water absorption
Limit: 3%-10%
Water Absorption Test of Aggregate: Lab Procedure, Result and Precautions - Dream Civil
2.1%-2.7%
N.A.≈ 1% (5%)

## Slide 12
The Treatment process reduces the initial quantity of fine particles included in RCA from 14% to 2%
Untreated RCA
Treated RCA
ASTM C117 Standard Test Method for Materials Finer than 75-μm (No. 200) Sieve in Mineral Aggregates by Washing

## Slide 13
Drainability is a significant consideration in roadway base materials
Increased pore water pressure
Reduction of strength/stiffness
Freeze-thaw damage
Treated RCA

## Slide 14
Critical parameter for long-term pavement structural integrity
NA : 27% (BNQ 2560-114/2002)
RCA : < 35% (BNQ 2002)

## Slide 15
Sustainable Development Goals
- Creation of specialized employment opportunities
- 40% increase in specialized training programs
60% diversion rate from landfills
- Enhanced urban infrastructure resilience
40-60% reduction in virgin material demand
- Promotion of circular economy principles
- 25-35% reduction in carbon emissions
- Decreased energy consumption in production
- 30-40% reduction in quarrying activities
- Enhanced ecosystem preservation

## Slide 16
Thank You